## Slide 1: Soft Lithography

## Slide 2: What is “Lab-on-a-Chip”?

## Slide 3: We will cover:
Designing a mask (I can help with this)
Making a master
  Surface preparation of wafer
  Photoresist
  Exposing of photoresist through mask
  Post exposure bake
PDMS Device
  Casting
  Punching holes
  PDMS Bonding
  Filling

## Slide 4: Designing a Mask
Designing a mask (I can help with this)
Making a master
  Surface preparation of wafer
  Photoresist
  Exposing of photoresist through mask
  Post exposure bake
PDMS Device
  Casting
  Punching holes
  PDMS Bonding
  Filling

## Slide 5: Designing a Mask
Free software:
    Layout Editor (we have monthly training)
    DraftSight
Shapes to be closed polygons.
Chrome masks with Heidelberg
    $200 flat rate ($300 commercial) from our mask shop
Polymask vendors (20um+):
  outputcity.com
  fineline-imaging.com

## Slide 6: Layout Editor

## Slide 7: DraftSight

## Slide 8: Making a Master
Designing a mask (I can help with this)
Making a master
  Surface preparation of wafer
  Photoresist
  Exposing of photoresist through mask
  Post exposure bake
PDMS Device
  Casting
  Punch holes
  PDMS Bonding
  Filling

## Slide 9: Making a Master
200C
100C
100C

## Slide 10: Surface Preparation
Designing a mask (I can help with this)
Making a master
  Surface preparation of wafer
  Photoresist
  Exposing of photoresist through mask
  Post exposure bake
PDMS Device
  Casting
  Punching holes
  PDMS Bonding
  Filling

## Slide 11: Substrate Surface Preparation
SU-8 Resist:
Make surface hydrophobic
  Silicon is hydrophobic, but SiO2 (due to exposure to atmospheric oxygen) is hydrophilic
Two possible treatments to promote adhesion:
  Removal of native oxide with HF (nasty)
  Prime wafer with HMDS in priming oven
Dehydration bake at 200C to drive off water molecules
KMPR Resist:
Dehydration bake at 200C only

## Slide 12: Photoresist
Designing a mask (I can help with this)
Making a master
  Surface preparation of wafer
  Photoresist
  Exposing of photoresist through mask
  Post exposure bake
PDMS Device
  Casting
  Punching holes
  PDMS Bonding
  Filling

## Slide 13: Negative Photoresist – How it works
Photoresist
Substrate
Mask

## Slide 14: Negative Photoresists
SU8-2000 series photosensitive epoxy
SU8-3000 series
KMPR-1000 series
QNF supplies SU8-2050, KMPR 1050

## Slide 15: Photoresist Spin Coating, Baking

## Slide 16: Exposure
Designing a mask (I can help with this)
Making a master
  Surface preparation of wafer
  Photoresist
  Exposing of photoresist through mask
  Post exposure bake
PDMS Device
  Casting
  Punching holes
  PDMS Bonding
  Filling

## Slide 17: Photoresist Exposure
Chart: Dose vs Thickness - KMPR
| 5 | 11 | 20 | 30 | 55 | 80
KMPR | 235 | 335 | 485 | 645 | 1055 | 1465

## Slide 18: Photoresist Exposure
ABM Mask Aligner

## Slide 19: Exposure Problems: Short Exposure
Result: delamination

## Slide 20: Exposure Problems: Long Exposure
Result: T-Topping
Solution: 360nm long pass filter

## Slide 21: Exposure Problems: Film Masks
Film masks have inherent defects not found in chrome masks

## Slide 22: Exposure Problems: Film Masks with 360LP filter
With 360LP filter
Without 360LP filter

## Slide 23: Exposure Problems: Film Masks with Thin Features
Chrome mask, 5um high features
Film mask, 5um high features
This problem is aggravated by the contrast caused by the LP filter.

## Slide 24: Post Exposure Bake
Designing a mask (I can help with this)
Making a master
  Surface preparation of wafer
  Photoresist
  Exposing of photoresist through mask
  Post exposure bake
PDMS Device
  Casting
  Punching holes
  PDMS Bonding
  Filling

## Slide 25: Post Exposure Bake Time

## Slide 26: PEB Problems: Thermal Stress
Stress cracks due to crosslinking and sudden temperature changes
Solutions:
Lower PEB temperature for longer bake time.
Annealing at 150C for 10 minutes after development

## Slide 27: PEB Problems: High Aspect Ratio Features
Delamination of high features with small footprints (related to thermal stress)
Solutions:
Better wafer preparation
Low PEB bake temperature
Annealing at 150C for 10 minutes after development

## Slide 28: PDMS
Designing a mask (I can help with this)
Making a master
  Surface preparation of wafer
  Photoresist
  Exposing of photoresist through mask
  Post exposure bake
PDMS Device
  Casting
  Punching holes
  PDMS Bonding
  Filling

## Slide 29: The Miracle of PDMS
Inexpensive 2-Part silicone elastomer
Hydrophobic native state
Surface of PDMS can be rendered hydrophilic with oxygen plasma
  Treatment last approximately 30 minutes
  Allows bonding to glass or to PDMS
  Allows functionalization of PDMS surface with hydrophilic molecules.
Gas permeable
Generally biocompatible, Food grade
Transparent in UV down to 240nm, ideal for fluorescence imaging
www.cchem.berkeley.edu
www.cchem.berkeley.edu
brandinside.deu

## Slide 30: Casting
Designing a mask (I can help with this)
Making a master
  Surface preparation of wafer
  Photoresist
  Exposing of photoresist through mask
  Post exposure bake
PDMS Device
  Casting
  Punching holes
  PDMS Bonding
  Filling

## Slide 31: PDMS Casting

## Slide 32: Punching Holes
Designing a mask (I can help with this)
Making a master
  Surface preparation of wafer
  Photoresist
  Exposing of photoresist through mask
  Post exposure bake
PDMS Device
  Casting
  Punching holes
  PDMS Bonding
  Filling

## Slide 33: Punch Holes (before bonding!)

## Slide 34: Tubing

## Slide 35: Bonding
Designing a mask (I can help with this)
Making a master
  Surface preparation of wafer
  Photoresist
  Exposing of photoresist through mask
  Post exposure bake
PDMS Device
  Casting
  Punching holes
  PDMS Bonding
  Filling

## Slide 36: Plasma Treatment for PDMS Bonding
PDMS-Glass: 50sccm O2, 30W, 30s (PDMS recipe)
PDMS-PDMS: 50sccm O2, 30W, 60s(PDMS-PDMS recipe)

## Slide 37: Filling
Designing a mask (I can help with this)
Making a master
  Surface preparation of wafer
  Photoresist
  Exposing of photoresist through mask
  Post exposure bake
PDMS Device
  Casting
  Punching holes
  PDMS Bonding
  Filling

## Slide 38: Filling
Priming the device soon after plasma bonding (within 3 hours) yields better results.
Fully submerging the device inside a vacuum chamber for 20 minutes yielded the best results.

## Slide 39: Preview of Hands-On Lab Work

## Slide 40: Soft Lithography Examples
Microfluidics
Stamping
Force Measurement

## Slide 41: Soft Lithography Examples
Microfluidics
Stamping
Force Measurement

## Slide 42: Soft Lithography Examples - Particle Separation

## Slide 43: Soft Lithography Examples – Gradient Generator

## Slide 44: Soft Lithography Examples – Cell Culture
Sugiura et al., Biotechnol. Bioeng. 100, 1156–1165 (2008)

## Slide 45: Soft Lithography Examples
Microfluidics
Stamping
Force Measurement

## Slide 46: Soft Lithography Examples - Stamping
Chen et al (1997) Science, 276:1425
DOI: 10.1126/science.276.5317.1425
Kamat et al (2013) Small, 9:2272
DOI: 10.1002/smll.201202627
Forced Cell Morphology
Vesicle Adhesion

## Slide 47: Soft Lithography Examples - Stamping
Schematic by Steven Henry

## Slide 48: Soft Lithography Examples
Microfluidics
Stamping
Force Measurement

## Slide 49: Soft Lithography Examples
Tan et al (2002) PNAS, 100:1484
DOI: 10.1073pnas.0235407100

## Slide 50: Questions?